## Slide 1: Step Dynamics in Homogeneous Crystal Growth
Matthew Koppa

## Slide 2: Many possibilities exist for an adatom diffusing over a terrace edge
1
Notes: Mention the three possibilities shown
Mention Schwoebel-Ehrlich barrier

## Slide 3: Study of crystal growth in homogeneous systems is relevant to many areas of current research
Microfabrication processes are at nanometer scales
Many of these devices are manufactured by growing crystals of a single element
Experimental results will provide a benchmark for theoretical models
2

## Slide 4: Study of diffusion at this level requires microscopy with atomic resolution
B.S. Swartzentruber, Phys. Rev. Lett. 76, 459 (1996).
3
Notes: Si dimer on an Si substrate (001) plane. Atom tracker STM image, black dots indicate lattice sites where the dimer hopped to
Right: FIM image of Ir that was taken with our FIM. Unsure of orientation ( figure that out by Monday)

## Slide 5: Field ion microscope (FIM) is well suited for the study of adatom diffusion
4
Notes: Why? Atomic resolution allows imaging of surface
specimen preparation naturally leads to the creation of many terrace edges (Rather than diffusion in a channel)
Single atom can be desorbed from the surface for analysis
Instrument can distinguish mass-to-charge ratio for the desorbed atom revealing it's identity
Segway, but before the specifics let's begin by discussing the theory of the FIM

## Slide 6: Field ionization and field evaporation require high electric fields
B. Gault et al., Atom Probe Microscopy, (Springer-Verlag, New York, NY, 2012)
5
Notes: Mention the axes. This is a graph of the potential energy of an electron in an atom, when the atom is near the surface of a metal
left is no field and right is field. Left, No possibility of tunneling because there are no available states to tunnel to
right, a large electric field raises the potential of the atom such that the electron can tunnel to an accessible state near the fermi level
Write this slide up carefully

## Slide 7: To produce a large electric field, specimens are shaped into needles
The tip of the needle is ~100 nm across
Electric field largest in regions with smallest radius of curvature
Electric field in the region of tip is ~1 V/Å
6
Notes: First mention the roughing done by electrochemical polishing.
Mention that the tip is fine polished in situ by field evaporation.
The tip is the metal from the previous slide. E-field is created by raising the dc voltage of the tip, segway: smash cut to...

## Slide 8: Positive ions allow the specimen to be imaged
Imaging gas ions are accelerated nearly normal to the surface
Collection of ions by microchannel plates allows specimen to be imaged at atomic resolution
B. Gault et al., Atom Probe Microscopy, (Springer-Verlag, New York, NY, 2012)
7

## Slide 9: Most protruding atoms create brightest spots
Ball model of a body centered cubic (BCC) crystal, (011) oriented, such as tungsten.
Outermost "atoms" painted with phosphorescent paint
8

## Slide 10: Field ion micrograph of iridium, a face centered cubic crystal (FCC), (100) oriented
Courtesy of J. Panitz
9

## Slide 11: Diagram of the essential features of a field ion microscope
10
Notes: Tip is mounted here. This is effectively every part of the FIM. Mention that this is purely schematic because it is a glass vaccuum system.
1. tip is mounted in UHV. Imaging gas in injected into the system. Reason for this is to create a large mean free path for the ions to travel to channel plates
Need to write up the total description for this slide
Mention the reasons for cooling (stopping diffusion, steadying the jitter for resolution, reducing lateral component of velocity for imaging ion)
Mention the deposition coil.
Why use a vacuum system?( Mean free path, no contaminants.)

## Slide 12: Diffusion studies in heterogeneous systems have been carried out using the FIM
Diffusion of Rh on W
G. Antczak and G. Ehrlich, Surface Diffusion: Metals, Metal Atoms, and Clusters, (Cambridge University Press, Cambridge, 2010).
11

## Slide 13: Exchange-mediated diffusion has been observed in heterogeneous systems
G. Antczak and G. Ehrlich, Surface Diffusion: Metals, Metal Atoms, and Clusters, (Cambridge University Press, Cambridge, 2010).
12

## Slide 14: Diffusion and step dynamics in homogeneous systems are more difficult to observe
Cannot distinguish exchange processes in systems with identical adatom and substrate atoms
Chemical nature of diffusing adatom affects step dynamics
Behavior of homogeneous adatoms should not be inferred from the heterogeneous case
13

## Slide 15: Atom probe allows measurement of mass-to-charge ratio of individual atoms via time-of-flight mass spectrometry
14

## Slide 16: Working version of atom probe is complete
15

## Slide 17: Adatom location determined using FIM
16

## Slide 18: Adatoms of interest may be off-center
17

## Slide 19: Adjustable specimen mount allows adatom to be aligned with detector
18

## Slide 20: Custom designed specimen mount has been manufactured and is installed on the system
Cold finger attaches to a welded bellows that can be adjusted to ensure adatom of interest is sent to detector
19

## Slide 21: Time of flight mass spectrometer
Atom of interest is field-evaporated and sent down drift tube
Mass-to-charge ratio distinguishes the identity of desorbed atom
20

## Slide 22: Procedure for studying adatom diffusion
Vacuum system is baked out to achieve ultra high vacuum pressures (~10^-10 torr)
Specimen tip is cooled to liquid nitrogen temperatures to stop diffusion
Adatoms are deposited onto tip
Imaging gas is backfilled into system
Tip is imaged using field ion microscope
Tip is heated to initiate diffusion
Tip is cooled to stop diffusion and image again
21

## Slide 23: Procedure for studying adatom diffusion (cont.)
If an interesting diffusion step has occurred the imaging channel plates are rotated out of the way and the system is evacuated
Detector channel plates are turned on and monitored by a photomultiplier tube (PMT)
A voltage pulse is applied to the tip to desorb the adatom from the surface
An oscilloscope is triggered by the pulse and records (PMT) voltage allowing time of flight measurements
22

## Slide 24: Use stable, isotopically enriched material to distinguish adatom/substrate atoms
W | Ir
180 < 1% | 191 37%
182 27% | 193 63%
183 14% | 
184 31% | 
186 28% | 
Available isotopes and isotopic abundance
23

## Slide 25: Repeated experiments generate sufficient statistics for the experiment
Even for substrates with a near 50-50 isotopic abundance, e.g. Ir, multiple trials allow adatom identification with a confidence level of 1 in 10^3
24

## Slide 26: Calculated time of flight measurements for 2+ and 3+ charge states of the stable isotopes of tungsten and iridium
Isotope | Abundance | Mass (u) | Time (microseconds), 2+ | Time (microseconds), 3+
W 180 | <1% | 179.95 | 8.84 | 7.22
W 182 | 27% | 181.95 | 8.89 | 7.26
W183 | 14% | 182.95 | 8.92 | 7.28
W184 | 31% | 183.95 | 8.94 | 7.30
W186 | 28% | 185.95 | 8.99 | 7.34
Ir 191 | 37% | 190.96 | 9.11 | 7.44
Ir 193 | 63% | 192.96 | 9.16 | 7.48
25

## Slide 27: Equation for finding mass-to-charge ratio from time of flight measurement from energy considerations
26

## Slide 28: Early results show the viability of the current atom probe
27

## Slide 29: Comparison with previously measured spectrum shows good agreement
A. Wagner et al., Rev. Sci. Instrum. 46, 1032 (1975).
28

## Slide 30: Many aspects of diffusion and step dynamics will be investigated
Diffusion along step edges
Dependence of step diffusion on particular crystallographic directions
Dependence of diffusion on terrace spacing
29

## Slide 31: Future instrument modifications may allow for investigation of non-equilibrium conditions
Using Joule heating the adatom reaches an equilibrium state between viewings
Pulsed laser heating could reveal intermediate steps
30

## Slide 32: Proposed project timeline
Tasks | Months during project
Construct atom probe | 1-6
Study adatom diffusion | 7-12
Investigate step dynamics | 7-12
Incorporate Laser heating | 13-15
Investigate step dynamics with and without laser heating | 13-24
Investigate possible step-step interactions | 25-36
31